B.E / B.Tech. PRACTICAL END SEMESTER EXAMINATIONS, APRIL / MAY 2019

Fourth Semester

CE8381 - STRENGTH OF MATERIALS AND FLUID MECHANICS & MACHINERY LABORATORY

(Regulations 2017)

Time : 3 Hours			       Answer any one Question	                      Max. Marks 100

| Aim/Principle/Apparatus required/Procedure | Tabulation/Circuit/Program/Drawing | Calculation & Results | Viva-Voce | Record | Total |
| --- | --- | --- | --- | --- | --- |
| 40 | 20 | 20 | 10 | 10 | 100 |

| 1. | Find the hardness of the given material using Brinell hardness testing machine. (i) aluminum (ii) Cast iron (iii) Mild steel |
| --- | --- |
| 2. | Perform the compression test on the given spring wire and find out its stiffness and rigidity modulus. |
| 3. | Using tension testing machine determine the yield stress, ultimate stress, breaking stress, percentage of reduction in area, percentage of elongation over a gauge length and young’s modulus for the given mild steel rod. |
| 4. | Find the strain measurement of given rod by using Rosette strain gauge. |
| 5. | Perform the torsion test on the given specimen to find the following 1. Modulus of rigidity 2. Shear stress. |
| 6. | Perform the heat treatment tempering on the given material C-40 steel and find its hardness. |
| 7. | Find hardness number and impact strength for unhardened, hardened specimen and Quenched and tempered specimen and compare mechanical properties. |
| 8. | Determine the mechanical properties of the given specimen (at least two samples to be given for each material) before and after hardening. |
| 9. | Examine the given specimens through microscope (before and after hardening) and draw the diagrams. Also comment on the effect of hardening based on the microscopic examination. |
| 10. | Determine the impact strength of the given specimen.(Charpy method). Find the shear strength of the given specimen under double shear method. |
| 11. | Determine the hardness of unhardened and quenched deep case hardened steel specimens by conducting Rockwell hardness test. |
| 12. | Determine the friction factor when the fluid flows through a15mm and 40mm diameter of the pipes. |
| 13. | Find the losses in pipes due to Sudden Enlargement, Sudden Contraction and bend for the given pipes. |
| 14. | Determine the Co-efficient of discharge through an Orifice by Constant Head Method |
| 15. | Determine the maximum efficiency and draw the performance characteristic Curves of Centrifugal Pump by using constant speed method. |
| 16. | Determine the maximum efficiency of Reciprocating Pump and draw the following graphs i. Discharge vs Head ii. Discharge vs input power iii. Discharge vs efficiency |
| 17. | Determine the performance of the Francis turbine, specific speed of the pump and Draw the constant head characteristic curves |
| 18. | Determine the performance of the Kaplan turbine, specific speed of The pump and draw the constant head characteristic curves. |
| 19. | Determine the efficiency of Pelton wheel and draw the performance Characteristic curves |
| 20. | Determine the maximum efficiency and draw the performance characteristic Curves by Gear Pump. |
| 21. | Perform an experiment to determine the flow in a pipe using venturimeter and determine the Co-efficient of discharge. |

INTERNAL EXAMINER						 EXTERNAL EXAMINER